SCOPE 142 ЛИ

Sofia, 21.04.2026

INDEPENDENT CONSTRUCTION LABORATORY INFRASTRUCTURE LTD.

INDEPENDENT CONSTRUCTION LABORATORY

Management and laboratory address:

1619, Sofia, Vitosha Municipality, 257 Tsar Boris III Blvd.

To perform testing of:

| Type of the scope: flexible* |  |  |  |
| --- | --- | --- | --- |
| № | Tested products | Type of test/characteristic | Testing methods (standard/ validated method) |
| 1 | 2 | 3 | 4 |
| 1. | Construction soils (unbound and hydraulically bound mixtures; aggregates for unbound and hydraulically bound mixtures for use in construction equipment and road construction) | 1.1 Determination of water content | БДС EN 1097–5; БДС EN ISO 17892-1 |
|  |  | 1.2 Determination of particle size distribution | БДС EN 933-1; БДС EN ISO 17892-4, cl. 5.2 and cl. 5.3 |
|  |  | 1.3 Determination of particle density | БДС EN ISO 17892-3, cl. 5.1 |
|  |  | 1.4 Determination of bulk density | БДС EN ISO 17892-2, cl. 5.1 and cl. 5.2; Appendix 18 of Ordinance № РД-02-20-2 |
|  |  | 1.5 Determination of dry density bulk density of the skeleton | БДС EN ISO 17892-2, cl. 5.1 and cl. 5.2; Appendix 18 of Ordinance № РД-02-20-2 |
|  |  | 1.6 Elastic module | БДС 15130 |
|  |  | 1.7 Deformation module | БДС 15130 |
|  |  | 1.8 Relation of deformation modules | БДС 15130 |
|  |  | 1.9 Determination of liquid limit | БДС EN ISO 17892-12, cl. 5.3; Appendix № 15 of Ordinance № РД-02-20-2 |
|  |  | 1.10 Determination of plastic limit Determination of liquid limit | БДС EN ISO 17892-12; Appendix № 16 of Ordinance № РД-02-20-2 |
|  |  | 1.11 Plasticity Index Plasticity Index | Appendix №16 of Ordinance № РД-02-20-2; БДC EN ISO 17892-12 |
|  |  | 1.12 Consistency Index | БДC EN ISO 17892-12 |
|  |  | 1.13 Determination of optimal water content | БДС 17146, cl. 3.3 – type of test Н 100, М 100, Н 150, М 150; БДС EN 13286-2, cl. 7.1, cl. 7.2, cl. 7.4, cl. 7.5, Appendix А |
|  |  | 1.14 Determination of normal density of the skeleton | БДС 17146, cl.3.3 – type of test Н 100, Н 150 |
|  |  | 1.15 Determination of modified density of the skeleton | БДС 17146, cl.3.3 – type of test М 100, М 150 |
|  |  | 1.16 Determination of degree of compaction | БДС 17146; Appendix № 18 of Ordinance № РД-02-20-2 |
|  |  | 1.17 Determination of the standard density of the skeleton – Proctor compaction | БДС EN 13286-2, cl. 7.1, cl. 7.2, Appendix А |
|  |  | 1.18 Determination of the standard density of the skeleton – modified Proctor compaction | БДС EN 13286-2, cl. 7.4; cl. 7.5, Appendix А |
|  |  | 1.19 Determination of California bearing ratio (CBR) | БДС EN 13286-47 |
|  |  | 1.20 Compression characteristics 1.20.1 Vertical deformation 1.20.2 Compression module 1.20.3 Coefficient of consolidation 1.20.4 Pore coefficient 1.20.5 Swelling pressure | БДС EN ISO 17892-5 |
|  |  | 1.21 Friction angle: - Peak friction angle, - Residual friction angle | БДС 10188, Amendment 1; БДС EN ISO 17892-10, cl. 4.1 |
|  |  | 1.22 Cohesion: - Peak cohesion, - Residual cohesion |  |
| 2. | Additives/Aggregates (coarse, fine / sand, fillers, unfractionated, for various applications | 2.1 Determination of particle size distribution | БДС EN 933-1 |
|  |  | 2.2 Determination of fine fraction content | БДС EN 933-1 |
|  |  | 2.3 Determination of California bearing ratio (CBR) | БДС EN 13286-47 |
|  |  | 2.4 Magnesium sulfate solution resistance | БДС EN 1367-2 |
|  |  | 2.5 Determination of bulk loose density | БДС EN 1097-3 |
|  |  | 2.6 Percentage of voids | БДС EN 1097-3; БДС EN 1097-6, cl. 7, cl. 8, cl. 9, Appendix В |
|  |  | 2.7 Determination of particle density: - Apparent particle density ρa, - Oven-dried particle density ρrd, - Saturated and surface-dried particle density ρssd, - Particle density of aggregates saturated to constant mass ρcm | БДС EN 1097-6, cl. 7, cl. 8, cl. 9, Appendix В |
|  |  | 2.8 Determination of water absorption | БДС EN 1097-6, cl. 7, cl. 8, cl. 9, Appendix В |
|  |  | 2.9 Shape index | БДС EN 933-4 |
|  |  | 2.10 Flakiness index | БДС EN 933- 3 |
|  |  | 2.11 Determination of: - Crushed particles, - Totally crushed particles, - Totally rounded particles | БДС EN 933-5 |
|  |  | 2.12 Determination of the length of particles | БДС EN 13450, cl. 6.7 |
|  |  | 2.13 Determination of the water content | БДС EN 1097-5 |
|  |  | 2.14 Resistance to fragmentation under static load | БДС EN 206+А2/NA (Appendix NA.Q) |
|  |  | 2.15 Determination of resistance to fragmentation - LA coefficient | БДС EN 1097-2 |
|  |  | 2.16 Percentage of shells | БДС EN 933-7 |
|  |  | 2.17 Sand equivalent | БДС EN 933-8+A1 |
|  |  | 2.18 Determination of the particle density of filler | БДС EN 1097-7 |
|  |  | 2.19 Determination of the voids of dry compacted filler | БДС EN 1097- 4 |
|  |  | 2.20 Determination of liquid limit | Appendix № 15 of Ordinance № РД-02-20-2 |
|  |  | 2.21 Determination of plastic limit | Appendix № 16 of Ordinance № РД-02-20-2 |
|  |  | 2.22 Plasticity index | Appendix № 16 of Ordinance № РД-02-20-2 |
|  |  | 2.23 Determination of the standard density of the skeleton – modified Proctor compaction | БДС EN 13286-2, cl. 7.4, cl. 7.5, Appendix А |
|  |  | 2.24 Determination of optimal water content | БДС EN 13286-2, cl. 7.4, cl. 7.5, Appendix А |
| 3. | Natural stone and rock aggregates | 3.1 Determination of particle bulk density | БДС EN 13383-2, cl. 8 |
|  |  | 3.2 Determination of water absorption | БДС EN 13383-2, cl. 8 |
|  |  | 3.3 Determination of dry compressive strength | БДС EN 1926 |
|  |  | 3.4 Determination of water-soaked compressive strength (for 48±4) h | БДС EN 1926, Appendix А |
| 4. | Bituminous mixtures | 4.1 Determination of bulk density of bituminous specimens | БДС EN 12697-6, Procedures А and В |
|  |  | 4.2 Determination of the maximum density | БДС EN 12697-5, Procedure А |
|  |  | 4.3 Residual voids Vm | БДС EN 12697-8, cl. 4 |
|  |  | 4.4 Soluble binder content | БДС EN 12697- 1, Appendix В, cl. В.2.1 |
|  |  | 4.5 Determination of particle size distribution | БДС EN 12697-2 |
|  |  | 4.6 Determination of stability by Marshall test | БДС EN 12697-34 |
|  |  | 4.7 Determination of the flow by Marshall test | БДС EN 12697-34 |
| 5. | Bitumens | 5.1 Penetration | БДС EN 1426 |
|  |  | 5.2 Elastic recovery | БДС EN 13398 |
|  |  | 5.3 Softening point | БДС EN 1427 |
| 6. | Concrete mixtures (1) Concrete (2) | 6.1 Slump test | БДС EN 12350-2 (1) |
|  |  | 6.2 Shape and dimensions of specimens | БДС EN 12390-1 (2) |
|  |  | 6.3 Compressive strength | БДС EN 12390-3 (2) |
|  |  | 6.4 Flexural strength | БДС EN 12390-5 (2) |
|  |  | 6.5 Tensile spliting strength | БДС EN 12390-6 (2) |
|  |  | 6.6 Watertightness 6.6.1 Water penetration depth | БДС EN 206+А2/NA (2) (Appendix NA.N) |
|  |  | 6.7 Frost resistance: - Relative mass loss, - Relative strength loss | БДС EN 206+А2/NA (2) (Appendix NA.O, Part NA.O.1 main method) |
|  |  | 6.8 Density of hardened concrete | БДС EN 12390 -7 (2) |
| 7. | Building structures (1), laid and compacted bituminous layers (2), waterproofing systems (3) | 7.1 Geometry of drill cores: - diameter – d, - height, - flatness, - straightness | БДС EN 12504-1 (1); БДС EN 12390-1 (1) |
|  |  | 7.2 Compressive strength of concrete from cut test specimens (cores) of prefabricated structures | БДС EN 12390-3 (1); БДС EN 12504-1 (1) |
|  |  | 7.3 Adhesion strength | # ASTM D 7234 (3) |
|  |  | 7.4 Determination of degree of compaction | БДС EN 12697- 9** (2) |
|  |  | 7.5 Determination of bulk density of bituminous specimens (core) | БДС EN 12697-6 (2), Procedures А and В |
|  |  | 7.6 Determination of the reference density | БДС EN 12697-9** (2) |
|  |  | 7.7 Determination of the thickness of bituminous pavement | # БДС EN 12697-36, cl. 6.1 (2) |
|  |  | 7.8 Benkelman beam deflection method | # БДС 15131 (2) |

To perform sampling of:

| Type of the scope: flexible* |  |  |
| --- | --- | --- |
| № | Product | Testing methods (standard/ validated method) |
| 1 | 2 | 3 |
| 1. | Construction soils (unbound and hydraulically bound mixtures; aggregates for unbound and hydraulically bound materials to be used in civil engineering work and road construction) | БДС EN 13286-1 |
| 2. | Additives/Aggregates (coarse, fine / sand, fillers, unfractionated, for various applications | БДС EN 932-1, cl. 8.8, Appendix А.2 |
| 3. | Bituminous mixtures | БДС EN 12697-27, cl. 4.1, cl. 4.3, cl. 4.7 |
| 4. | Concrete mixtures, concrete | БДС ЕN 12350-1 |
| 5. | Building structures (1), laid and compacted bituminous layers (2) | БДС ЕN 12504-1, cl. 6 (1); БДС EN 12697-27, cl. 4.7 (2) |

Flexible scope: *The introduction of a new version of the standards/documents or standards/documents that superseded them shall be permited. The laboratory maintains an updated list of standards/documents with their dated versions.

** Repealed standard but not superseded in terms of test metod.

Reference:

Ordinance № РД-02-20-2 of 28.08.2018 г. on road design of the Ministy of regional Development and Public Works (prom. SG № 79 of 2018, Amd. SG № 90 of 2018, effective as of 26.10.2018); Appendix № 15, Appendix № 16, Appendix № 18.