SCOPE 182 ЛИ

Sofia, 11.06.2025

STROYCONTROL 2003 LTD.

CONSTRUCTION TESTING LABORATORY

Management address: 1505 Sofia, 45 Kalimantsi Str, Office 3

Laboratory address: 1612 Sofia, Krasno selo, 12 Kostenets Str.

To perform testing of:

| Type of the scope: flexible |  |  |  |
| --- | --- | --- | --- |
| № | Tested products | Type of test / characteristic | Testing methods (standard / validated) |
| 1 | 2 | 3 | 4 |
| 1. | Aggregates for concrete (1) Aggregates for mortar (2) Aggregates for bituminous mixtures (3) Aggregates for unbound and hydraulically bound mixtures (4) | 1.1. Particle size distribution | БДС EN 933-1 (1,2,3,4) |
|  |  | 1.2 Sand equivalent | БДС ЕN 933–8 (1,2,3,4) |
|  |  | 1.3. Shape index | БДС EN 933-4 ( 1,3,4) |
| 2. | Fresh concrete (1) and hardened concrete (2) | 2.1. Slump | БДС EN 12350-2 (1) |
|  |  | 2.2. Density | БДС EN 12390-7 (2) |
|  |  | 2.3. Compressive strength | БДС EN 12390-3 (2) |
|  |  | 2.4.Freeze-thaw resistance | БДС EN 206-1+А2/NA(2) |
|  |  | 2.5. Water permeability/Depth of water penetration under pressure | БДС EN 206-1+А2/NA(2) БДС EN 12390-8 (2) |
|  |  | 2.6. In situ compressive strength | БДС EN 12504-1 (2) |
| 3. | Steel for reinforcement of concrete structures. Weldable reinforcing steel (1) Welded fabric and lattice girders. (2) | 3.1. Mass per unit length | БДС EN ISO 15630-1 (1,2) |
|  |  | 3.2. Yield strength | БДС EN ISO 6892-1 (1,2) |
|  |  | 3.3. Tensile strength/Force at break | БДС EN ISO 6892-1 (1,2) |
|  |  | 3.4. Elongation at break -A5 | БДС EN ISO 6892-1 (1,2) БДС EN ISO 15630-1 (1,2) |
|  |  | -Agt | БДС EN ISO 15630-1 (1,2) |
|  |  | 3.5. Shear force | БДС EN ISO 15630-2 (2) |

To perform sampling of:

| Type of the scope: flexible |  |  |
| --- | --- | --- |
| № | Product | Sampling methods (standard/validated method) |
| 1 | 2 | 3 |
| 1. | Fresh concrete | БДС EN 12350-1 Testing fresh concrete – Part 1: Sampling |

Flexible scope: Implementing a new version of standards/documents or standards/ documents replacing them is allowed. An updated list of standards/documents and their dated versions is provided by CAB.