SCOPE 10 ЛК

Kalabsi Ltd.

Calibration laboratory Kalabsi

Management and laboratory address: 1505 Sofia, 7 Neofit Bozveli Str.

To perform calibrating of:

| Type of the scope: flexible for part of the scope |
| --- |
| № | Measuring instrument | Measured value unit of measure | Measurement Range | Uncertainly of measurement | Calibration method |
| 1 | 2 | 3 | 4 | 5 | 6 |
| 1. | Machines (equipment, devices and apparatus) for testing materials and products of tension / compression | Force, N tension/ compression, | from 0,5 N to 1000 N | 0,3 % | РПК 702 С 01 |
|  |  |  | from 1 kN to 1000 kN | 0,5 % |  |
|  |  |  | from 1000 kN to 2000 kN | 0,6 % |  |
| 2. | Dynamometers | Force, N tension/ compression, | from 0,5 N to 1000 N | 0,2 % | РПК 702 С 02 |
|  |  |  | from 1 kN to 1000 kN | 0,3 % |  |
|  |  |  | from 1000 kN to 2000 kN | 0,4 % |  |
| 3. | Pendulum-type impact testing machines (Charpy hammer) | Energy J, | from 0,1 J to 450 J | from 1,3 % to 0,5 % | РПК 702 Е 01 |
| 4. | Torque wrenches | Torque, Nm | from 0,4 Nm to 1100 Nm | 1,0 % | РПК 702 М 01 |
| 5. | Reference hardness blocks using the method of Brinell | Hardness /the method of Brinell/ HBW | from 90 HBW to 400 HBW | 2,0 % | РПК 702 Т 01 |
| 6. | Reference hardness blocks using the method of Rockwell, scales A, B and C | Hardness /the method of Rockwell/ HRA HRВ HRС | from 60 HRA to 88 HRA | 0,8 HRA | РПК 702 Т 01 |
|  |  |  | from 60 HRВ to 100 HRВ | 0,8 HRB |  |
|  |  |  | from 20 HRС to 70 HRС | 0,8 HRС |  |
| 7. | Reference hardness blocks using the method of Vickers – second level | Hardness /the method of Vickers/ HV | from 200 HV to 800 HV (from HV 1 to HV 30) | 2,0 % | РПК 702 Т 01 |
| 8. | Hardness testers using the method of Brinell (stationary and portable) | Hardness /the method of Brinell/ HBW | from 90 HBW to 400 HBW | 2,0 % | РПК 702 Т 02 |
| 9. | Hardness testers using the method of Rockwell, scales A, B and C (stationary and portable) | Hardness /the method of Rockwell/ HRA HRВ HRС | from 60 HRA to 88 HRA | 1,0 HRA | РПК 702 Т 02 |
|  |  |  | from 60 HRВ to 100 HRВ | 1,0 HRB |  |
|  |  |  | from 20 HRС to 70 HRС | 1,0 HRС |  |
| 10. | Hardness testers using the method of Vickers (stationary and portable) | Hardness /the method of Vickers/ HV | from 200 HV to 800 HV (from HV 1 to HV 30) | 2,0 % | РПК 702 Т 02 |
| 11. | Dial gauge for length measurement | Length m | up to 1,0 mm | 1,5 (m | РПК 702 Д 01 |
|  |  |  | up to 25 mm | 3,0 (m |  |
| 12. | Line scales and measuring tapes. | Length m | for tapes and tape measures to 5000 mm | 0,6 mm | РПК 702 Д 02 |
|  |  |  | for lines to 1500 mm |  |  |
| 13. | Calipers | Length m | up to 250 mm | 0,03 mm | РПК 702 Д 03 |
| 14. | Micrometers, for 2-point external and internal dimensions | Length m | up to 100 mm | 1,3 (m | РПК 702 Д 04 |
| 15. | Pressure measuring devices | Pressure, bar | from -0,95 bar to 0 bar with air | 0,3% FS | РПК 702 Н 01 |
|  |  |  | up to 2,5 bar with air | 0,1% FS |  |
|  |  |  | up to 600 bar with oil |  |  |

*Note: The measuring devices are calibrated at the customer's site.

Flexible scope: Implementing a new version of standards/documents or standards/ documents replacing them is allowed. An updated list of standards/documents and their dated versions is provided by the laboratory.

References:

- РПК 702 C 01 Calibration of systems for measuring the force of machines for testing materials and products of tension/compression (based on БДС EN ISO 7500-1);

- РПК 702 C 02 Calibration of dynamometers (based on БДС EN ISO 376);

- РПК 702 Е 01 Calibration of energy measurement system for hammer bending test machines (Charpy hammer) (based on БДС EN ISO 148-2);

- РПК 702 М 01 Calibration of torque wrenches (based on БДС EN ISO 6789);

- РПК 702 Т 01 Calibration of reference hardness blocks – second level by the methods of Brinell, Rockwell and Vickers (based on БДС EN ISO 6506-3, БДС EN ISO 6507-3, and БДС EN ISO 6508-3);

- РПК 702 Т 02 Calibration of hardness testers by the methods of Brinell, Rockwell and Vickers (based on БДС EN ISO 6506-2, БДС EN ISO 6507-2 and БДС EN ISO 6508-2);

- РПК 702 Д 01 Calibration of dial gauges for length measurement (2018);

- РПК 702 Д 02 Calibration of line scales and measuring tapes (2018);

- РПК 702 Д 03 Calibration of caliper devices (2018);

- РПК 702 Д 04 Calibration of micrometer devices (2018);

- РПК 702 Н 01 Calibration of pressure measuring devices (based on EURAMET cg-17) (2020).