SCOPE 222 ЛИ

Construction testing laboratory

at Evropat 2005 Ltd, Haskovo

Management address: 6300 Haskovo, 14 Kozloduy Str, floor 5

Laboratory address: 6300 Haskovo, Suchukmaz Area, Asphalt base

To perform testing of:

| Type of the scope: Flexible |  |  |  |
| --- | --- | --- | --- |
| № | Tested products | Type of test / characteristic | Testing methods (standard / validated method) |
| 1 | 2 | 3 | 4 |
| 1. | Aggregate/rock materials: Rock materials for bituminous mixtures and paving of roads, runways and other areas (1.1) concrete admixtures (1.2) Mineral flour for asphalt concrete mixtures (1.3) Crushed stone for railway lines (1.4) Rock materials for unbound and hydraulically bound mixtures for use in civil engineering and road construction - Construction soils (1.5) | 1.1. Grain size composition | БДС EN 933-1 (1.1; 1.2; 1.3; 1.4; 1.5) БДС 2880, cl. 2.1.3 (1.3) БДС 2762, cl. 1 (1.5) |
|  |  | 1.2. Fine fraction content (below 0.063 mm sieve) | БДС EN 933-1 (1.1; 1.2; 1.4; 1.5) |
|  |  | 1.3. Sand equivalent | БДС EN 933-8+A1 (1.1; 1.2; 1.5) |
|  |  | 1.4. Form factor | БДС EN 933-4 (1.1; 1.2; 1.4) |
|  |  | - Percentage of: - entirely crushed grains - crushed grains - entirely rounded grains | БДС EN 933-5 (1.1; 1.2; 1.4) |
|  |  | - Grain density - absolute grain density; - grain density in dry condition; -grain density in a water-saturated surface dry condition; | БДС EN 1097-6 (1.1; 1.2; 1.4) |
|  |  | 1.7. Shell contents | БДС EN 933-7 (1.2) |
|  |  | 1.8. Water absorption | БДС EN 1097-6 (1.1; 1.2; 1.4) |
|  |  | 1.9. Volatilization resistance to magnesium sulfate | БДС EN 1367-2 (1.1; 1.2; 1.4; 1.5) |
|  |  | 1.10. Water content | БДС EN 1097-5 (1.1; 1.2; 1.3; 1.4; 1.5) |
|  |  | 1.11. Humidity | БДС 2880, cl. 2.1.4 (1.3) |
|  |  | 1.12. Water content | БДС 644* (1.5) |
|  |  | 1.13. Yield strength | Ordinance № РД-02-20-2 on road design, issued by the MRDPW Appendix № 15 |
|  |  | 1.14. Drainage limit; Plasticity index | Ordinance № РД-02-20-2 on road design, issued by the MRDPW Appendix № 16 |
| 2. | Asphalt mixtures | 2.1. Bulk density | БДС EN 12697-6 |
|  |  | 2.2. Maximum density | БДС EN 12697-5 |
|  |  | 2.3. Air pore content (VA) | БДС EN 12697-8, cl. 4 |
|  |  | 2.4. Marshall Test: - stability; - flow | БДС EN 12697-34 |
|  |  | 2.5. Soluble binder content | БДС EN 12697-1 |
|  |  | 2.6. Particle size distribution | БДС EN 12697-2+A1 |
|  |  | 2.7. Compaction degree | БДС EN 12697-9* |
|  |  | 2.8. Mixture temperature | БДС EN 12697-13 |
|  |  | 2.9. Water content | БДС EN 12697-14 |
|  |  | - Dimensions of the tested body: - diameter; - height; - width | БДС EN 12697-29 |
|  |  | 2.11. Asphalt pavement thickness | БДС EN 12697-36, cl. 4.1 |
| 3. | Bitumen and bituminous binders | 3.1. Penetration | БДС EN 1426 |
|  |  | 3.2. Softening temperature subject to ring and ball method | БДС EN 1427 |
|  |  | 3.3. Adhesion between mineral/rock material and bitumen | БДС EN 11685 БДС EN 12697-11, cl. 7 |

To perform sampling of:

| Scope Type: Flexible |  |  |
| --- | --- | --- |
| № | Name of the tested products | Test methods (standardized/validated) |
| 1 | 2 | 3 |
| 1. | Rock materials for bituminous mixtures and paving of roads, runways and other areas; Concrete admixtures; Mineral flour for asphalt concrete mixtures; Crushed stone for railway tracks; | БДС EN 932-1 |
| 2. | Rock materials for unbound and hydraulically bound mixes for use in construction equipment and road construction/ Construction soils | БДС EN 932-1 БДС EN 13286-1 |
| 3. | Asphalt mixtures | БДС EN 12697-27 |
| 4. | Bitumen and bituminous binders | БДС EN 58 |

* Repealed but not replaced standard with regard to the testing method.

Flexible scope: Implementing a new version of standards/documents or standards/ documents replacing them is allowed. An updated list of standards/documents and their dated versions is provided by laboratory.

References:

Ordinance № РД-02-20-2, on road design, issued by MRDPW, Appendix № 15, Appendix № 16.