SCOPE 270 ЛИ

of Groma Hold Ltd.

Construction testing laboratory

Management address:

2709 Belo Pole, Production Plant of Groma Hold Ltd.

Laboratory addresses:

STATIONARY OFFICE (Office 1): 2709 Belo Pole, Poleto Location,

Production Plant of Groma Hold Ltd.

MOBILE OFFICE (Office 2): 3100 Mezdra, 92A Hristo Botev Str.

I. STATIONARY OFFICE (Office 1):

2709 Belo Pole, Poleto Location, Production Plant of Groma Hold Ltd.

To perform testing of:

| Type of scope: flexible |
| --- |
| № | Tested products | Type of test / characteristic | Testing methods (standard / validated methods) |
| 1 | 2 | 3 | 4 |
| 1. | Aggregates | 1.1. | Particle size distribution | БДС EN 933-1 |
|  |  | 1.2. | Fines content | БДС EN 933-1 |
|  |  | 1.3. | Percentage of: - totally crushed particles; - crushed particles; - totally rounded particles; | БДС EN 933-5 |
|  |  | 1.4. | Overall flakiness index | БДС EN 933-3 |
|  |  | 1.5. | Shape index | БДС EN 933-4 |
|  |  | 1.6. | Sand equivalent | БДС EN 933-8+A1 |
|  |  | 1.7. | Methylene blue value | БДС EN 933-9 |
|  |  | 1.8. | Coefficient – Micro Deval | БДС EN 1097-1 |
|  |  | 1.9. | Coefficient – Los Angeles | БДС EN 1097-2 |
|  |  | 1.10. | Resistance to fragmentation | БДС EN 206+А2/NA, annex NA.Q |
|  |  | 1.11. | Мass loss during cyclic freezing - thawing | БДС EN 1367-1 |
|  |  | 1.12. | Magnesium sulfate value | БДС EN 1367-2 |
|  |  | 1.13. | Loose bulk density. Percentage of voids. | БДС EN 1097-3 |
|  |  | 1.14. | Particle density - apparent particle density; - oven-dried particle density; - saturated and surface-dried article density - pre-dried particle density; - particle density saturated to constant mass | БДС EN 1097-6 clause 7, 8, 9 Annex А - clause А.3, А.4 Annex В |
|  |  | 1.15. | Water absorption | БДС EN 1097-6 clause 7, 8, 9 Annex В |
|  |  | 1.16. | Degree of bitumen coverage (Affinity between aggregate and bitumen) | БДС EN 12697-11, Boiling water stripping method |
|  |  | 1.17. | California bearing ratio /CBR/ | БДС EN 13286-47 |
|  |  | 1.18. | Maximum density of the skeleton. Optimum water content | БДС EN 13286-2 |
|  |  | 1.19. | Water content | БДС EN 1097-5 |
|  |  | 1.20. | Plastic limit. Plasticity index. | AASHTO T 90 Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 16 to article 160, item 3* БДС EN ISO 17892-12 |
|  |  | 1.21. | Liquid limit | AASHTO T89 Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 15 to article 160, item 3* БДС EN ISO 17892-12, Casagrande method |
|  |  | 1.22. | Presence of humus | БДС EN 1744-1+A1 |
|  |  | 1.23. | Percentage of lightweight particles | БДС EN 1744-1+A1 |
|  |  | 1.24. | Deformation module | Ordinance 55, art. 47 |
| 2. | Filler | 2.1. | Particle size distribution | БДС EN 933-1 |
|  |  | 2.2. | Methylene blue value | БДС EN 933-9+А1 |
|  |  | 2.3. | Water content | БДС EN 1097-5 |
|  |  | 2.4. | Loose bulk density | БДС EN 1097-3 |
|  |  | 2.5. | Voids | БДС EN 1097-4 |
|  |  | 2.6. | Particle density | БДС EN 1097-7 |
| 3. | Bituminous mixtures | 3.1. | Particle size distribution | БДС EN 12697-2+А1 |
|  |  | 3.2. | Soluble binder content | БДС EN 12697-1 |
|  |  | 3.3. | Bulk density | БДС EN 12697-6 |
|  |  | 3.4. | Indirect tensile strength | БДС EN 12697-23 |
|  |  | 3.5. | Indirect tensile strength ratio | БДС EN 12697-12, method A |
|  |  | 3.6. | Dimensions of asphalt test specimen | БДС EN 12697-29 |
|  |  | 3.7. | Maximum density | БДС EN 12697-5 |
|  |  | 3.8. | Air voids content | БДС EN 12697-8 |
|  |  | 3.9. | Stability | БДС EN 12697-34 |
|  |  | 3.10. | Flow | БДС EN 12697-34 |
|  |  | 3.11. | Binder drainage | БДС EN 12697-18, Beaker method |
|  |  | 3.12. | Temperature | БДС EN 12697-13 |
|  |  | 3.13. | Voids content in the mineral aggregate | БДС EN 12697-8 |
|  |  | 3.14. | Percentage of voids in the mineral aggregate filled with binder | БДС EN 12697-8 |
| 4. | Bitumens | 4.1. | Penetration | БДС EN 1426 |
|  |  | 4.2. | Softening point | БДС EN 1427 |
|  |  | 4.3. | Elastic recovery | БДС EN 13398 |
|  |  | 4.4. | Flash point | БДС EN ISO 2592 |
|  |  | 4.5. | Resistance to hardening RTFOT method: - retained penetration at 25 оС - change in softening point - change in mass | БДС EN 12607-1 |
|  |  | 4.6. | Fraass breaking point | БДС EN 12593 |
|  |  | 4.7. | Storage stability -difference in the softening point of top and bottom layer. | БДС EN 13399 |
|  |  | 4.8. | Density | БДС EN 15326+A1 |
|  |  | 4.9. | Solubility | БДС EN 12592 |
|  |  | 4.10. | Deformation energy by the force ductility method | БДС EN 13589 |
| 5. | Fresh concretes | 5.1. | Slump | БДС EN 12350-2 |
|  |  | 5.2. | Slump – Vebe test | БДС EN 12350-3 |
|  |  | 5.3 | Density | БДС EN 12350-6 |
| 6. | Concrete | 6.1. | Compressive strength | БДС EN 12390-3 БДС EN 12504-1 |
|  |  | 6.2. | Flexural strength | БДС EN 12390-5 |
|  |  | 6.3. | Tensile splitting strength | БДС EN 12390-6 |
|  |  | 6.4. | Density | БДС EN 12390-7 |
|  |  | 6.5. | Depth of penetration of water under pressure | БДС EN 12390-8 |
|  |  | 6.6. | Resistance to frost during direct freezing and thawing: - Relative loss of mass; - Relative loss of strength; | БДС EN 206+А2/NA, annex NA.O |
|  |  | 6.7. | Rebound number | БДС EN 12504-2 |
| 7. | Cement | 7.1. | Strength | БДС EN 196-1 |
|  |  | 7.2. | Setting time | БДС EN 196-3 |
|  |  | 7.3. | Soundness | БДС EN 196-3 |
|  |  | 7.4. | Standard consistency | БДС EN 196-3 |
| 8. | Construction soils | 8.1. | Particle size distribution | AASHTO T 88 БДС EN 933-1 |
|  |  | 8.2. | Fines content | БДС EN 933-1 |
|  |  | 8.3. | Plastic limit. Plasticity index. | БДС EN ISO 17892-12 AASHTO T90 Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 16 to article 160, item 3* |
|  |  | 8.4. | Liquid limit | БДС EN ISO 17892-12 - Casagrande method AASHTO T89 Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 15 to article 160, item 3* |
|  |  | 8.5. | Maximum density of the skeleton. Optimum water content | БДС 17146 БДС EN 13286-2 |
|  |  | 8.6. | California bearing ratio /CBR/ | БДС EN 13286-47 |
| 9. | Earth and rock embarkments and foundations (base layers) | 9.1. | Elastic module | БДС 15130 |
|  |  | 9.2. | Deformation module | БДС 15130 |
|  |  | 9.3. | Deformation modules ratio | БДС 15130 |
|  |  | 9.4. | Bulk density of the skeleton by the sand-replacement method. Compaction degree. | Ordinance № РД-02-20-2, SG № 79/2018 •Annex № 18* |
| 10. | Road pavements | 10.1. | Thickness of asphalt layer | БДС EN 12697–36, Destructive method |
|  |  | 10.2. | Compaction degree | БДС EN 12697-9** |
|  |  | 10.3. | Irregularities of pavement course | БДС EN 13036-7 |
|  |  | 10.4. | Bulk density of asphalt test specimen (core) | БДС EN 12697-6 |
|  |  | 10.5. | Conventional reference density | БДС EN 12697-9** |
| 11. | Concrete elements | 11.1. | Dimensions |  |
|  |  |  | - paving blocks | БДС EN 1338/AC |
|  |  |  | - paving flags | БДС EN 1339/AC |
|  |  |  | - kerb units | БДС EN 1340/AC |
|  |  | 11.2. | Splitting strength | БДС EN 1338/AC |
|  |  | 11.3. | Water absorptions |  |
|  |  |  | - paving blocks | БДС EN 1338/AC |
|  |  |  | - paving flags | БДС EN 1339/AC |
|  |  |  | - kerb units | БДС EN 1340/AC |
|  |  | 11.4. | Bending strength - paving flags - kerb units | БДС EN 1339/AC БДС EN 1340/AC |
| 12. | Waterproofings | 12.1. | Adhesion pull-off strength | ASTM D7234 |
|  |  | 12.2. | Tensile strength | Technical Rules on the Design and Technology for the Construction of the Waterproofing of Reinforced Concrete Bridges of the Chief Office Roards dated 1997, Annex 1 |
| 13. | Unbound mixtures | 13.1. | Particle size distribution | БДС EN 933-1 |
|  |  | 13.2. | Fines content | БДС EN 933-1 |
|  |  | 13.3. | Water content | БДС EN 1097-5 |
|  |  | 13.4. | Maximum bulk density of the skeleton. Optimum water content | БДС EN 13286-2 БДС 17146 |
|  |  | 13.5. | California bearing ratio | БДС EN 13286-47 |
|  |  | 13.6. | Magnesium sulfate value | БДС EN 1367-2 |
|  |  | 13.7. | Plastic limit. Plasticity index. | БДС EN ISO 17892-12 AASHTO T90 Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 16 to article 160, item 3* |
|  |  | 13.8. | Liquid limit | БДС EN ISO 17892-12 - Casagrande method AASHTO T89 Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 15 to article 160, item 3* |
|  |  | 13.9. | Elastic module. Deformation module. Deformation modules ratio | БДС 15130 |
| 14. | Hydraulically bound mixtures | 14.1. | Particle size distribution | БДС EN 933-1 |
|  |  | 14.2. | Water content | БДС EN 1097-5 |
|  |  | 14.3. | Maximum bulk density of the skeleton. Optimum water content | БДС EN 13286-2 БДС 17146 |
|  |  | 14.4. | Compressive strength | БДС EN 13286-41 |
|  |  | 14.5. | Laying time (workability period) | БДС EN 13286-45 |
|  |  | 14.6. | California bearing ratio | БДС EN 13286-47 |
|  |  | 14.7. | Immediate bearing index | БДС EN 13286-47 |
|  |  | 14.8. | Linear swelling | БДС EN 13286-47 |
|  |  | 14.9. | Bulk density of the skeleton by the sand-replacement method | Ordinance № РД-02-20-2 •Annex № 18* |
|  |  | 14.10. | Compaction degree | Ordinance № РД-02-20-2 •Annex № 18* |

# To perform sampling of:

| Type of scope: flexible |
| --- |
| № | Product | Sampling methods (standard / validated methods) |
| 1 | 2 | 3 |
| 1. | Aggregates | БДС EN 932-1 – sampling from stockpiles |
| 2. | Filler | БДС EN 932-1 – sampling from stockpiles and with and with sampling tube (spear) |
| 3. | Bituminous mixtures | БДС EN 12697-27 – sampling from a lorry load of material |
| 4. | Bitumens | БДС EN 58 – sampling from the surface of road tankers |
| 5. | Construction soils | БДС EN 932-1 – sampling from stockpiles |
| 6. | Fresh concretes | БДС EN 12350-1 |
| 7. | Cement | БДС EN 196-7 – sampling of cement from bulk transport (after loading or before unloading) |
| 8. | Road pavements | БДС EN 12697-27 – sampling of laid and compacted materials by coring |
| 9. | Concrete elements | БДС EN 1338/AC |
|  |  | БДС EN 1339/AC |
|  |  | БДС EN 1340/AC |
| 10. | Concrete | БДС EN 12504-1 |
| 11. | Unbound mixtures | БДС EN 932-1 – sampling from stockpiles |
| 12. | Hydraulically bound mixtures | БДС EN 932-1 – sampling from stockpiles |

II. MOBILE OFFICE (Office 2): 3100 Mezdra, 92 A Hristo Botev Str.

To perform testing of:

| Type of scope: flexible |
| --- |
| № | Tested products | Type of test / characteristic | Testing methods (standard / validated methods) |
| 1 | 2 | 3 | 4 |
| 1. | Aggregates | 1.1. | Particle size distribution | БДС EN 933-1 |
|  |  | 1.2. | Fines content | БДС EN 933-1 |
|  |  | 1.3. | Overall flakiness index | БДС EN 933-3 |
|  |  | 1.4. | Shape index | БДС EN 933-4 |
|  |  | 1.5. | Sand equivalent | БДС EN 933-8+A1 |
|  |  | 1.6. | Particle density - apparent particle density; - oven-dried particle density; - saturated and surface-dried article density - pre-dried particle density; - particle density saturated to constant mass | БДС EN 1097-6 clause 7, 8, 9 Annex А - clause А.3, А.4 Annex В |
|  |  | 1.7. | Water absorption | БДС EN 1097-6 clause 7, 8, 9 Annex В |
|  |  | 1.8. | California bearing ratio /CBR/ | БДС EN 13286-47 |
|  |  | 1.9. | Maximum density of the skeleton. Optimum water content | БДС EN 13286-2 |
|  |  | 1.10. | Съдържание на вода | БДС EN 1097-5 |
|  |  | 1.11. | Plastic limit. Plasticity index. | Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 16 to article 160, item 3* БДС EN ISO 17892-12 |
|  |  | 1.12 | Liquid limit | Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 15 to article 160, item 3* БДС EN ISO 17892-12, Casagrande method |
|  |  | 1.13. | Deformation module | Ordinance 55, art. 47 |
| 2. | Bituminous mixtures | 2.1. | Particle size distribution | БДС EN 12697-2+А1 |
|  |  | 2.2. | Soluble binder content | БДС EN 12697-1 |
|  |  | 2.3. | Bulk density | БДС EN 12697-6 |
|  |  | 2.4. | Dimensions of asphalt test specimen | БДС EN 12697-29 |
|  |  | 2.5. | Maximum density | БДС EN 12697-5 |
|  |  | 2.6. | Air voids content | БДС EN 12697-8 |
|  |  | 2.7 | Stability | БДС EN 12697-34 |
|  |  | 2.8. | Flow | БДС EN 12697-34 |
|  |  | 2.9. | Temperature | БДС EN 12697-13 |
| 3. | Bitumens | 3.1. | Penetration | БДС EN 1426 |
|  |  | 3.2. | Softening point | БДС EN 1427 |
|  |  | 3.3. | Elastic recovery | БДС EN 13398 |
| 4. | Fresh concretes | 4.1. | Slump | БДС EN 12350-2 |
|  |  | 4.2 | Density | БДС EN 12350-6 |
| 5. | Construction soils | 5.1. | Particle size distribution | БДС EN 933-1 |
|  |  | 5.2. | Fines content | БДС EN 933-1 |
|  |  | 5.3. | Plastic limit. Plasticity index. | Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 16 to article 160, item 3* |
|  |  | 5.4. | Liquid limit | Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 15 to article 160, item 3* |
|  |  | 5.5. | Maximum density of the skeleton. Optimum water content | БДС 17146 БДС EN 13286-2 |
|  |  | 5.6. | California bearing ratio /CBR/ | БДС EN 13286-47 |
| 6. | Earth and rock embarkments and foundations (base layers) | 6.1. | Elastic module | БДС 15130 |
|  |  | 6.2. | Deformation module | БДС 15130 |
|  |  | 6.3. | Deformation modules ratio | БДС 15130 |
|  |  | 6.4. | Bulk density of the skeleton by the sand-replacement method. Compaction degree. | Ordinance № РД-02-20-2, SG № 79/2018 •Annex № 18* |
| 7. | Road pavements | 7.1. | Thickness of asphalt layer | БДС EN 12697–36, Destructive method |
|  |  | 7.2. | Compaction degree | БДС EN 12697-9** |
|  |  | 7.3. | Irregularities of pavement course | БДС EN 13036-7 |
|  |  | 7.4. | Bulk density of asphalt test specimen (core) | БДС EN 12697-6 |
|  |  | 7.5. | Conventional reference density | БДС EN 12697-9** |
| 8. | Unbound mixtures | 8.1. | Particle size distribution | БДС EN 933-1 |
|  |  | 8.2. | Fines content | БДС EN 933-1 |
|  |  | 8.3. | Water content | БДС EN 1097-5 |
|  |  | 8.4. | Maximum bulk density of the skeleton. Optimum water content | БДС EN 13286-2 БДС 17146 |
|  |  | 8.5. | California bearing ratio | БДС EN 13286-47 |
|  |  | 8.6. | Magnesium sulfate value | БДС EN 1367-2 |
|  |  | 8.7. | Plastic limit. Plasticity index. | БДС EN ISO 17892-12 Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 16 to article 160, item 3* |
|  |  | 8.8. | Liquid limit | БДС EN ISO 17892-12 - Casagrande method Ordinance № РД-02-20-2, SG № 79/2018 • Annex № 15 to article 160, item 3* |
|  |  | 8.9. | Elastic module. Deformation module. Deformation modules ratio | БДС 15130 |
| 9. | Hydraulically bound mixtures | 9.1. | Particle size distribution | БДС EN 933-1 |
|  |  | 9.2. | Water content | БДС EN 1097-5 |
|  |  | 9.3. | Maximum bulk density of the skeleton. Optimum water content | БДС EN 13286-2 БДС 17146 |
|  |  | 9.4. | California bearing ratio | БДС EN 13286-47 |
|  |  | 9.5. | Immediate bearing index | БДС EN 13286-47 |
|  |  | 9.6. | Linear swelling | БДС EN 13286-47 |
|  |  | 9.7. | Bulk density of the skeleton by the sand-replacement method | Ordinance № РД-02-20-2, Annex № 18* |
|  |  | 9.8. | Compaction degree | Ordinance № РД-02-20-2, Annex № 18* |

To perform sampling of:

| Type of scope: flexible |
| --- |
| № | Name of product | Method of sampling (standard / validated methods) |
| 1 | 2 | 3 |
| 1. | Aggregates | БДС EN 932-1 – sampling from stockpiles |
| 2. | Bituminous mixtures | БДС EN 12697-27 – sampling from a lorry load of material |
| 3. | Bitumens | БДС EN 58 – sampling from the surface of road tankers |
| 4. | Construction soils | БДС EN 932-1 – sampling from stockpiles |
| 5. | Fresh concretes | БДС EN 12350-1 |
| 6. | Road pavements | БДС EN 12697-27 – sampling of laid and compacted materials by coring |
| 7. | Concrete | БДС EN 12504-1 |
| 8. | Unbound mixtures | БДС EN 932-1 – sampling from stockpiles |
| 9. | Hydraulically bound mixtures | БДС EN 932-1 – sampling from stockpiles |

Flexible scope: Implementing a new version of standards/documents or standards / documents replacing them is allowed. An updated list of standards/documents and their dated versions is provided by laboratory.

** БДС EN 12697-9:2004 is repealed but not replaced standard with regard to the testing method.

*References:

MRDPW Ordinance № РД-02-20-2, SG № 79/2018,

•Annex № 15 to art. 160, item 3: Method for determination of liquid limit of soils;

MRDPW Ordinance № РД-02-20-2, SG № 79/2018,

•Annex № 16 to art. 160, item 3: Method for determination of plastic limit and plasticity index of soils;

MRDPW Ordinance № РД-02-20-2, SG № 79/2018,

•Annex № 18 to art. 168, para. 1: Method for determining the bulk density of construction soils in situ by substitute sand.