SCOPE 152 ЛИ

of Stroicontrol SP Ltd.

Construction Testing Laboratory

Management and laboratory address:

1390 Sofia, Filipovtsi, 10A, Hadzhi Dimitar Str.

To perform testing of:

| Type of the scope: flexible** |  |  |  |
| --- | --- | --- | --- |
| № | Tested products | Type of test / characteristic | Testing methods (standard / validated method) |
| 1 | 2 | 3 | 4 |
| 1. | Concrete mixes | 1.1 Slump-test | БДС EN 12350-2 |
|  |  | 1.2 Density | БДС EN 12350-6 |
|  |  | 1.3 Air content | БДС EN 12350-7 |
| 2. | Concrete | 2.1 Hardened concrete density | БДС EN 12390-7 |
|  |  | 2.2 Compressive strength | БДС EN 12390-3 |
|  |  | 2.3 Tensile splitting strength | БДС EN 12390-6 |
|  |  | 2.4 in-situ compressive strength in structures and precast concrete components | БДС ΕΝ 13791/NA |
|  |  | 2.5 Water-tightness | БДС ΕΝ 206+A1/NA, Annex NA.N |
|  |  | 2.6 Depth of penetration of water under pressure | БДС EN 12390-8 |
|  |  | 2.7 Frost resistance - relative loss of mass - ultrasound impulse velocity reduction | БДС ΕΝ 206+A2/NA, Annex ΝΑ.O cl. ΝΑ.O.2.6. |
|  |  | 2.8 Carbonation depth of hardened concrete | БДС EN 14630 |
| 3. | Aggregates for concretes (1); Rock materials for bitumen mixes and pavements, unbound and hydraulically bound mixes for building structures and road construction (2); Unbound and hydraulically bound mixes for building structures and road construction (3); Rock materials for hydro-technical construction (4); Rock materials for railway lines (5); | 3.1 Particle size distribution | БДС EN 933-1 |
|  |  | 3.2 Content of fine fraction with sieve size 0,063mm | БДС EN 933-1 (1,2,3) |
|  |  | 3.3 Inequigranularity index d60/d10 | БДС ΕΝ 13242+A1/NA, |
|  |  | 3.4 Flakiness index | БДС EN 933-3 |
|  |  | 3.5 Shape index | БДС EN 933-4 |
|  |  | 3.6 Determination of percentage of particles with crushed and broken surfaces | БДС EN 933-5 (1,2,3) |
|  |  | 3.7 Sand equivalent | БДС EN 933-8+А1 (1,2,3) |
|  |  | 3.8 Loose bulk density | БДС EN 1097-3 (1,2,3) |
|  |  | 3.9 Resistance to fragmentation of the coarse aggregate under static load | БДС ΕΝ 206+A1/NA, Annex NA.Q |
|  |  | 3.10 Water content | БДС EN 1097-5 |
|  |  | 3.11 Particle density and water absorption ρσ; ρrd; ρssd; WA24; | БДС EN 1097-6 |
|  |  | 3.12 Standard bulk density with optimum water content. Proctor compaction - normal and modified | БДС EN 13286-2 (3,4) |
|  |  | 3.13 Compressive strength of hydraulically bound mixtures | БДС EN 13286-41 (3) |
|  |  | 3.14 California bearing ratio (CBR) | БДС EN 13286-47 (3) |
|  |  | 3.15 Elastic modulus Ееср | БДС 15130-80 (3,4) |
|  |  | 3.16 Deformation modulus: 2. E01 3. Е02 4. Е03 | БДС 15130-80 (3,4) |
|  |  | Deformation modulus ratio Е01/ E02 |  |
|  |  | 3.17 Plate load test settlement | БДС EN 1997-2 Annex К |
|  |  | 3.18 Liquid limit | Ordinance № РД-02-20- 2* Annex № 15 to Art. 160, item 3 AASHTO Т 89 |
|  |  | 3.19 Plastic limit | Ordinance № РД-02-20- 2* Annex № 16 to Art. 160, item 3 AASHTO Т 90 |
|  |  | 3.20 Plasticity indicator | Ordinance № РД-02-20- 2* Annex № 16 to Art. 160, item 3 AASHTO Т 90 |
|  |  | 3.21 Dry density | AASHTO Т 191 (3,4) |
|  |  | 3.22 Wet density | AASHTO Т 191 (3,4) |
|  |  | 3.23 Compaction index | AASHTO Т 191 (3,4) |
| 4. | Building soils | 4.1 Water content | БДС EN ISO 17892-1 AASHTO Т191 |
|  |  | 4.2 Particle size distribution | БДС EN 933-1 БДС EN ISO 17892-4 |
|  |  | 4.3 Inequigranularity index d60/d10 | БДС EN ISO 14688-2 |
|  |  | 4.4 Bulk density | БДС EN ISO 17892-2 |
|  |  | 4.5. Dry density | БДС EN ISO 17892-2 |
|  |  | 4.6 California bearing ratio (CBR) | БДС EN 13286-47 |
|  |  | 4.7 Standard bulk density with optimum water content. Proctor compaction - normal and modified | БДС EN 13286-2 |
|  |  | 4.8 Elastic modulus Ееcp | БДС 15130-80 |
|  |  | 4.9 Deformation modulus: 5. E01 6. Е02 7. Е03 | БДС 15130-80 |
|  |  | Deformation modulus ratio Е02/ Е01 |  |
|  |  | 4.10 Plate load test settlement | БДС EN 1997-2, Annex К |
|  |  | 4.11 Dry Density | AASHTO Т191 |
|  |  | 4.12 Wet density | AASHTO Т 191 |
|  |  | 4.13 Compaction index | AASHTO Т 191 |
| 5. | Applied and compacted asphalt | 5.1 Bulk density of asphalt core sample | БДС EN 12697-6 |
|  |  | 5.2 Asphalt layer thickness - destructive method | БДС EN 12697-36 |

To perform sampling of:

| Type of the scope: flexible** |  |  |
| --- | --- | --- |
| № | Product | Sampling method (standard/validated) |
| 1 | 2 | 3 |
| 1. | Concrete mixes | БДС EN 12350-1 |
| 2. | Concrete | БДС EN 12504-1 |
| 3. | Aggregates for concretes. Rock materials for bitumen mixes and pavements; for unbound and hydraulically bound mixes; for building structures and road construction; for hydro-technical construction; for railway lines | БДС EN 932-1 |
| 4. | Rock materials for unbound and hydraulically bound mixes | БДС ΕΝ 13286-1 |
| 5. | Building soils | БДС ΕΝ 13286-1 |

**Flexible scope: Implementing a new version of standards/documents or standards / documents replacing them is allowed. An updated list of standards/documents and their dated versions is provided by CAB.

*References:

1) Annex № 15 to Art. 160, item 3 of Ordinance № РД-02-20-2/28.08.2018 for road design of the Ministry of Regional Development and Public Works, SG № 79/25.09.2018.

2) Annex № 16 to Art. 160, item 3 of Ordinance № РД-02-20-2/28.08.2018 for road design of the Ministry of Regional Development and Public Works, SG № 79/25.09.2018.