SCOPE 158 ЛИ

Sofia, 23.01.2024

of Texnotest Ltd.

Construction testing laboratory

Management and laboratory address:
3000 Vratsa, 10, Aleko Konstantinov Str.

To perform testing of:

| № | Tested products | Type of test / characteristic | Testing methods (standard / validated method) |
| --- | --- | --- | --- |
| 1 | 2 | 3 | 4 |
| 1. | Aggregates /dense aggregates for concrete, sand for concrete, sand for construction mortars, sand for bituminous mixtures for use in road construction, aggregates for bituminous mixtures and surface treatments for roads, airfields and other trafficked areas, aggregates for unbound and hydraulically bound materials for use in civil engineering work and road construction, aggregates for railway construction/ | 1.1. Particle size distribution | БДС EN 933-1 |
|  |  | 1.2. Shape index | БДС EN 933-4 |
|  |  | 1.3 Percentage of: - crushed particles; - totally crushed particles; - totally rounded particles; | БДС ЕN 933-5 |
|  |  | 1.4 Percentage of shell content | БДС ЕN 933-7 |
|  |  | 1.5 Resistance to fragmentation – “Los Angeles” coefficient | БДС ЕN 1097-2 |
|  |  | 1.6 Loose bulk density / Percentage of voids | БДС ЕN 1097-3 |
|  |  | 1.7 Water content | БДС ЕN 1097-5 |
|  |  | 1.8 Particle density | БДС ЕN 1097-7 |
|  |  | 1.9 Water absorption | БДС 12159 |
|  |  | 1.10 Resistance to wear – “micro-Deval” coefficient | БДС EN 1097-1 |
|  |  | 1.11 Abrasion resistance | БДС ЕN 14157 |
|  |  | 1.12 Magnesium sulfate value (Mass loss by testing with magnesium sulfate - resistance to frost) | БДС ЕN 1367-2 |
|  |  | 1.13 Sand equivalent | БДС EN 933-8+А1 |
|  |  | 1.14 Resistance to fragmentation | БДС EN 206+A2/NA, NA.Q |
|  |  | 1.15 Methylene blue value | БДС EN 933-9 |
|  |  | 1.16 Particle density: - apparent particle density; - oven-dried particle density; - saturated and surface-dried particle density; - pre-dried particle density; | БДС ЕN 1097-6, cl. 7, cl. 8, cl. 9, Annex A |
|  |  | 1.17 Water absorption | БДС ЕN 1097-6, cl. 7, cl. 8, cl. 9, Annex B БДС ЕN 13755 |
|  |  | 1.18 Compressive strength | БДС ЕN 1926 |
|  |  | 1.19 Overall flakiness index | БДС EN 933-3 |
|  |  | 1.20 Fines content | БДС EN 933-1 |
|  |  | 1.21 Content of fine particles | БДС EN 933-1 БДС EN 13450+AC, cl. 6.4 |
|  |  | 1.22 Particle’s length | БДС EN 13450+AC, cl. 6.7 |
|  |  | 1.23 Uniformity coefficient | БДС EN ISO 14688-2 |
| 2. | Fresh concrete | 2.1 Slump | БДС ЕN 12350-2 |
|  |  | 2.2 Density | БДС ЕN 12350-6 |
| 3. | Hardened concrete | 3.1 Compressive strength | БДС ЕN 12390-3 БДС ЕN 12504-1 |
|  |  | 3.2 Density | БДС ЕN 12390-7 |
|  |  | 3.3 Water impermeability | БДС EN 206+A2/ NA, NA.N |
|  |  | 3.4 Resistance to frost /direct freezing and thawing/ | БДС EN 206+A2/NA, NA.O.1 |
|  |  | 3.5 Rebound number | БДС EN 12504-2 |
| 4. | Construction soils | 4.1 Density in-place by the sand-cone method | AASHTO T191 |
|  |  | 4.2 Water content | БДС 644* БДС EN ISO 17892-1 БДС EN ISO 17892-1/A1 |
|  |  | 4.3 Specific gravity / Particle density | БДС 646* БДС EN ISO 17892-3, fluid pycnometer method |
|  |  | 4.4 Bulk density / Dry density | БДС EN ISO 17892-2, linear method with cylindrical specimen |
|  |  | 4.5 Coefficient of pores | БДС EN ISO 14688-2 |
|  |  | 4.6 Maximum bulk density of skeleton / Optimum water content | БДС 17146 /cl. 3.3.1 and cl. 3.3.2/ БДС EN 13286-2 /method A and В/ |
|  |  | 4.7 Liquid limit / Plastic limit | БДС 648* БДС EN ISO 17892-12, MRDPW, Ordinance № РД-02-20-2, Annex №15**; MRDPW, Ordinance № РД-02-20-2, Annex №16** |
|  |  | 4.8 Compressive properties | БДС EN ISO 17892-5 БДС 8992* |
|  |  | 4.9 Direct shear strength | БДС 10188 |
|  |  | 4.10 Coefficient of water permeability | БДС 8497, БДС EN ISO 17892-11, testing with rigid wall permeameter |
|  |  | 4.11 Particle size distribution | БДС EN 933-1 БДС EN ISO 17892-4 |
|  |  | 4.12 Elastic module / Deformation modules / Deformation modules ratio | БДС 15130 |
|  |  | 4.13 California bearing ratio - CBR | БДС EN 13286-47 MRDPW, Ordinance № РД- 02-20-2, Annex № 17** |
|  |  | 4.14 Dynamic probing - penetration under the influence of a standard dynamic penetrometer-type light (DPL light) | БДС EN ISO 22476-2+A1 |
|  |  | 4.15 Degree of compaction | AASHTO T191 MRDPW, Ordinance № РД- 02-20-2, Annex № 18** БДС 17146 |
|  |  | 4.16 Degree of water saturation | БДС 2761*, cl. 3.1.4 |
|  |  | 4.17 Plasticity index | БДС 2761*, cl. 3.2.4 БДС EN ISO 17892-12, cl. 6.5; MRDPW, Ordinance № РД- 02-20-2, Annex № 16** |
|  |  | 4.18 Consistency index | БДС 2761*, cl. 3.2.5 БДС EN ISO 17892-12, Annex B, cl. Bl.2 |
|  |  | 4.19 Loose bulk density / Percentage of voids | БДС EN 1097-3 |
|  |  | 4.20 Volume of macro-pores | БДС 2761*, cl. 2.8 БДС 14783 |
|  |  | 4.21 Particle density: - apparent particle density; - oven-dried particle density; - saturated and surface-dried particle density; pre-dried particle density; | БДС EN 1097-6, cl. 7, cl. 8, cl. 9, Annex A |
|  |  | 4.22 Water absorption | БДС EN 1097-6, cl. 7, cl. 8, cl. 9, Annex B |
|  |  | 4.23 Fines content | БДС EN 933-1 |
|  |  | 4.24 Sand equivelent | БДС EN 933-8+A1 |
|  |  | 4.25 Resistance to wear - "micro-Deval" coefficient | БДС EN 1097-1 |
|  |  | 4.26 Resistance to fragmentation - "Los Angeles" coefficient | БДС EN 1097-2 |
|  |  | 4.27 Bulk density by the sand replacement method / Bulk density if skeleton by the sand replacement method | MRDPW, Ordinance № РД- 02-20-2, Annex №18** |
| 5. | Bituminous mixtures | 5.1 Bulk density /initial bulk density, reference bulk density/ | БДС ЕN 12697-6 |
|  |  | 5.2 Maximum bulk density | БДС ЕN 12697-5 |
|  |  | 5.3 Compaction degree | БДС EN 12697-9* |
|  |  | 5.4 Stability / Flow | БДС ЕN 12697-34 |
|  |  | 5.5 Soluble binder content | БДС ЕN 12697-1 |
|  |  | 5.6 Particle size distribution | БДС ЕN 12697-2+A1 |
|  |  | 5.7 Indirect tensile strength ratio (Water sensibility) | БДС ЕN 12697-12 |
|  |  | 5.8 Air voids content | БДС ЕN 12697-8 |
|  |  | 5.9 Temperature | БДС EN 12697-13 |
|  |  | 5.10 Dimensions of a bituminous specimen: - height; - diameter; | БДС EN 12697-29 |
|  |  | 5.11 Thickness of a bituminous layer | БДС EN 12697-36 destructive measurement |
|  |  | 5.12 Indirect tensile strength | БДС EN 12697-23 |
|  |  | 5.13 Irregularity of pavement's surface | БДС EN 13036-7 |
| 6. | Flexible sheets for waterproofing. Waterproofing of concrete bridge decks and other concrete surfaces trafficable by vehicles | 6.1 Bond strength | БДС EN 13596 TRDTCWRCB, Annex 1** |

To perform sampling of:

| № | Product | Sampling methods (standardized / validated) |
| --- | --- | --- |
| 1 | 2 | 3 |
| 1 | Aggregates | БДС EN 932-1 |
| 2 | Fresh concrete | БДС EN 12350-1 |
| 3 | Hardened concrete | БДС EN 12504-1 |
| 4 | Bituminous mixtures | БДС EN 12697-27 |
| 5 | Construction soils | БДС EN 932-1 |

* Repealed but not replaced standard with regard to the testing method.

Flexible scope: Implementing a new version of standards/documents or standards / documents replacing them is allowed. An updated list of standards/documents and their dated versions is provided by the CAB.

Flexible scope references:

** Annex № 15:  Method for determination of liquid limit of soils to Art. 160, item 3 of Ordinance № РД-02-20-2/28.08.2018 on road design of Ministry of Regional Development and Public Works /MRDPW/, SG № 79/2018, amd. SG № 90/2018, valid from 26.10.2018;

** Annex № 16: Method for determination of plastic limit and plasticity index of soils to Art. 160, item 3 of Ordinance № РД-02-20-2/28.08.2018 on road design of Ministry of Regional Development and Public Works /MRDPW/, SG № 79/2018, amd. SG № 90/2018, valid from 26.10.2018;

** Annex № 17:  Method for determining of California Bearing Ratio of soil (CBR) to Art. 161, table 39 and Art. 162, table 40 of Ordinance № РД-02-20-2/28.08.2018 on road design of Ministry of Regional Development and Public Works /MRDPW/, SG № 79/2018, amd. SG № 90/2018, valid from 26.10.2018;

** Annex № 18 Method for determining of bulk density of construction soils by the sand replacement method to Art. 161, table 39 and Art. 162, table 40 of Ordinance № РД-02-20-2/28.08.2018 on road design of Ministry of Regional Development and Public Works /MRDPW/, SG № 79/2018, amd. SG № 90/2018, valid from 26.10.2018;

** Technical Rules on the Design and Technology for the Construction of the Waterproofing of Reinforced Concrete Bridges of the Chief Office Roads: TRDTCWRCB: 1997. Annex 1.